3QSAB 09-608

August 25, 2009

Supersedes

3FNE 98-572D

May 2, 2005

Purchase Description

Technical Requirements for Wood Executive Office,
Conference Room/Casegoods Furniture and
Single Item Accent and Specialty Pieces

Intended use:  Furniture shall be marketed for executive use.  Furniture is intended for use by Government executives (or equivalent military rank) in the Executive, Judicial, Legislative Branches or Armed Forces of the Federal Government.

Minimum construction requirements:  Furniture shall comply with one of the grades of construction/materials and one of the three design categories explained below.  GSA assigns grades and design categories based on the information in the Construction Material Data (CMD) sheets provided with the offer.

The GSA National Furniture Center established a grading method to help customers identify the furniture construction/materials desired.  The grading method consists of a grade for the casegood chassis, and a separate grade for the drawers.  In addition, the GSA National Furniture Center established three design categories to help our customers make a purchasing decision based on their needs and budget.

Grades of furniture construction/materials.  Furniture lines and drawer construction in Grade 1 includes wood furniture that tends to be the most expensive of this group, and Grades 2, 3 and 4 wood furniture tends to be progressively more affordably priced when compared to Grade 1.

All pieces with a GSA Chassis Grade 1-3 shall have wood veneered or solid wood chassis and top (unless otherwise noted below). Design features such as leather, burl, veneer border, inlay, marquetry, stone, glass and metal accents are acceptable for all chassis grades.  Leather, glass, marble/stone or solid surface tops are acceptable in lieu of wood tops in GSA Chassis grades 1 through 3.  High-pressure laminate tops are acceptable only as an option in GSA Chassis grades 1 through 3.

If a particular line of furniture or drawer construction has properties which fall into different GSA Grades, the furniture line or drawer construction will be assigned a grade of the lowest property (e.g. if the edgeband thickness earns a grade 3, but the Base Rail construction earns a grade 2, the furniture will receive a GSA Chassis Grade 3).

Design categories:

- Traditional. Encompasses styles such as Queen Anne, Georgian (such as Chippendale, Hepplewhite, Sheraton and Adam) and Neo-Classical.

- Transitional. Contemporary design with the influence of period styling without being heavy or bulky in appearance.

- Contemporary. Light, clean, simple geometric shapes, functional style that depends on good finish and design rather than ornamental decoration.

------------------------------------------------------------------------------------------------------------------

Catalog Requirements.  The contractor shall include the entire Italics text of the Grade of Furniture Construction/Materials and Design Categories sections of this document, in a prominent type face, at the beginning of the section in the contract catalog (printed and on-line versions) covering this furniture.  In addition, each line or series of this furniture shall have the GSA grade designation and design category listed beside each line name/number both in the price list and color brochure (printed and on-line versions).  For example, “Series 2000, GSA Grade (1), Traditional Design”.

Construction Material Data Sheet.  All offerors are required to complete a Construction Material Data (CMD) sheet for each line or piece, if item is offered individually, of office furniture submitted.  A blank copy of the CMD sheet is included at the end of this purchase description.  If a line is offered in more than one wood species, a separate CMD sheet shall be completed for each wood species.  The CMD sheet along with commercial brochures/catalogs will be used in determining the acceptability of lines/pieces offered and in determining which grade and design the furniture will be classified in.

| GSA CHASSIS CONSTRUCTION GRADES |
| --- |
| Components | Grade 1 (Solid) | Grade 1 (Veneer) | Grade 2 (Veneer) | Grade 3 (Veneer) |
| Exposed wood parts/panels other than base rails | Panels and parts shall be solid wood of the same species. Contrasting wood species permitted for decorative accents and inlays. | Veneered panels and wood parts shall be of the same species. Contrasting wood species permitted for decorative accents and inlays. | ← Same as grade 1 | Mixed wood species permitted for panels and parts. Wood grained composite trim molding permitted. |
| Exposed wood base rails | Solid wood shall be the same species as other exposed parts. | Wood shall be the same species as other exposed parts. | Alternative wood species permitted. | ← Same as grade 3 |
| Exposed interior material (e.g. kneespaces, bookcase interiors, interiors behind doors) | Wood shall be the same species as other exposed parts. | ← Same as Grade 1 | ← Same as Grade 1 | Applied material with an appearance that matches the color and grain of exposed panels on rest of case is permitted. |
| Exposed wood edgeband thickness | N/A | Min. 3 mm (tops and end panels) | Min. 3 mm (tops only) | Less than 3 mm |

GSA Chassis Grade (N/A)  Base/chassis/frame may be materials such as exposed brass, chrome, stainless steel, marble/stone.  Top/shelves may be materials such as wood, wood veneered panel, glass, marble/stone, solid surface material.  Materials such as laminate, vinyl and printed surfaces are not acceptable in this chassis grade.

| GSA DRAWER CONSTRUCTION GRADES Precision ball bearing suspensions required on all drawers. |
| --- |
| Components | Grade 1 | Grade 2 | Grade 3 | Grade 4 |
| Drawer fronts | Solid wood or veneered panel with min. 3 mm thick exposed wood edgeband. | Veneered panel with exposed wood veneer edgeband or visible lumber core. | Veneered panel with foil edgeband or edges finished to match face. | ← Same as Grade 3 |
| Drawer sides and backs | Solid hardwood (excluding lauan) | Hardwood veneer core plywood. | Hardwood plywood with composite core and banded top edges, or solid lauan lumber. | Composite core with decorative overlay or steel drawer box |
| Drawer bottoms | Suitable core with hardwood veneer face | ← Same as Grade 1 | Suitable core with wood grained decorative overlay | Composite core with decorative overlay or steel drawer box |

Performance Testing.  Products offered are required to meet the following industry standards or GSA test method in effect on the date of issuance of the solicitation.  In addition, during the contract period, product manufactured must meet the applicable standards, in effect at the time of manufacture.  If the test standard is revised during the term of the contract, the manufacturer will be required to retest in accordance with the new standard.  Copies of the referenced documents may be obtained from the issuing organizations at the addresses shown.

If a dispute arises relating to testing, GSA reserves the right to determine whether a test is appropriate for the product offered.

Items that shall be tested.  The following test requirements apply to all furniture lines being offered for all construction grades.

- Casegood items such as desks and credenzas shall meet all applicable test sections in the most current edition ANSI/BIFMA X5.5 (Desk Product Test).  One representative worst case item (e.g. the largest item offered, item with largest drawers, item with most drawers) shall be tested from each line of furniture, provided all of the other pieces in the line have the same construction, materials and drawer suspensions.  If other pieces in the line have different model drawer suspensions or different construction, they must be tested as well.  For example, if you are offering furniture line XYZ that is made up of various sizes of double pedestal desks, L-unit work stations and credenzas, that all have the same model box and file drawer suspensions and the same construction, only the largest single pedestal desk would have to be tested.

- Lateral File Cabinets shall meet all applicable test sections in the most current edition of ANSI/BIFMA X5.9 (Storage Unit Tests).  One representative worst case item (the widest unit with the greatest number of drawers offered) shall be tested from each line of furniture, provided all of the other lateral files in the line have the same construction, materials and drawer suspensions.  If other lateral files in the line have different model drawer suspensions or different construction, they must be tested as well.

- Work Tables/Table Desks shall meet all applicable test sections in the most current edition of ANSI/BIFMA X5.5 (Desk Product Test).  One representative worst case item (the largest item offered) shall be tested from each line of furniture, provided all of the other work tables/table desks in the line have the same construction, materials and drawer suspensions.  If other work tables/table desks in the line have different model drawer suspensions or different construction, they must be tested as well.

- Oblong Conference Room Tables shall meet all applicable test sections in the most current edition ANSI/BIFMA X5.5 (Desk Product Test).  One representative worst case table offered (the table(s) with the longest span between supports) shall be tested from each line of furniture, provided all of the other oblong tables in the line have the same construction and materials.  If oblong tables in the line have different base designs (leg, panel etc.), each base design must be tested as well.  If an oblong table line is offered with different shape tops, (rectangular, oval, race track, boat) only one of the top shapes needs to be tested.

- Round Conference Room Tables shall meet all applicable test sections in the most current edition ANSI/BIFMA X5.5 (Desk Product Test).  One representative worst case table offered (the table with the largest diameter) shall be tested from each line of furniture, provided all of the other round tables in the line have the same construction and materials.  If round tables in the line have different base designs (leg, pedestal etc.), each base design shall be tested as well.

- Bookcases shall meet all applicable test sections in the most current edition of ANSI/BIFMA X5.9 (Storage Units).  In addition, the following Bookcase shelf static load deflection test shall be performed.  One representative worst case item (the widest unit with the greatest number of shelves offered) shall be tested from each line of furniture, provided all of the other bookcases in the line have the same construction, materials and shelf support method.  If bookcases that are structurally the same are offered in multiple lines with only changes in trim, only one version is required to be tested.

- Tall Storage Units with Vertically Attached or Stackable Components shall meet 8.1 Disengagement test in most current edition of ANSI/BIFMA X5.9.  One representative worst case tall storage unit with vertically attached or stackable components offered (the tallest, apparently least stable unit) shall be tested from each line of furniture, provided all of the other units in the line have the same construction and materials.  If other units in the line have different attachment methods, these units shall be tested as well.

Bookcase shelf static load deflection test.

Preparation:  Place complete bookcase on a flat, level surface.  Install shelves in bookcase, evenly spaced top to bottom.  Place a 9 kg mass on both ends of each shelf for 5 minutes to ensure that the shelf supports are fully engaged.  Remove these masses.  Place dial indicators or equivalent measuring devices at the front edge of the bookcase top panel and each shelf.  Take initial readings.

Test:  Apply an evenly distributed load as identified in the functional load requirement in Table 1 of ANSI/BIFMA X5.9 on the bookcase top panel and each shelf at the same time.  Maintain forces for 30 minutes.  Record deflections with masses in place.  Remove masses.

Acceptance level:  Maximum deflection for the top and each shelf while masses are in place:  the deflection shall not exceed L/180 for the shelf and top length.  End panels shall not bow while masses are in place.  Structural damage to the case, shelves or shelf supports that affect serviceability or could cause personal injury to the user is not acceptable. Before and after testing, shelves and top shall have a maximum sag or warp of L/1000 for the shelf and top length.

Test Reporting and Certification Requirements.  Manufacturers must provide a test certification stating that the products offered have been tested and have passed the applicable test requirements.  The certification must be included with the offer.  The manufacturer shall retain test reports used as the basis for the certification for the term of the contract.  GSA reserves the right to request copies of test reports at any time prior to contract award or during the course of the contract.  Failure to provide test reports may result in rejection of the offer or termination of the contract.

As a minimum, the test certification shall be submitted on company letterhead and shall include the following information:

- The manufacturer’s name and model number of the item tested, or if appropriate, the product line tested.

- Date or range of dates that the test(s) were performed.

- A statement that testing and certification apply to the product offered and that products offered meet all applicable test requirements.

- Signature, date, and title of the company official accepting technical responsibility for testing.

Age of Tests and Test Certifications.  Test certifications must be current and based on performance test reports not more than three years old at time of submittal of offer.  All performance test reports and certifications must be updated when they are five years old, when performance test method is revised, or if any product changes occur during the five-year period. It is the supplier’s responsibility to track the age of test results and test certifications.  When the five year age limit is approaching, the supplier shall retest and recertify his products and provide the certifications to the contracting officer so that by the five year mark, acceptable test certifications will be in place.

If the manufacturer is ISO 9001 registered and the tests were performed while the manufacturer was ISO 9001 registered, performance tests are valid for the term of the contract unless changes have been made to the product or test standard.  A copy of the offeror’s ISO 9001 registration showing compliance must be submitted with the reports/certifications. Manufacturers that become registered during the term of the contract must complete one successful test sequence after the registration.

Product changes include changes to the construction/design.  Changes in materials and hardware (except drawer suspensions) are acceptable without additional testing provided they continue to meet the same specifications as those used on the unit that was tested.

For example if the furniture manufacturer changed particleboard suppliers but the new particleboard still had the same density and met the same performance requirements as the original product, the unit would not need to be retested.  If however, the panel material was changed from veneer core to particleboard core plywood, the representative unit would have to be retested.  If drawer suspensions are changed, the representative unit would have to retested regardless of what the performance characteristics of the new drawer suspensions are.  Whenever a unit is to be retested a new test certification shall be submitted to the contracting officer.

Who may perform tests.  Tests shall either be performed ”in house” by the furniture manufacturer or shall be performed by an independent test lab.  We encourage furniture manufacturers making offers under this solicitation to become ISO 9001 certified.  ISO documents may be obtained from the American National Standards Institute, 25 West 43rd Street, 4th floor, New York, New York 10036, (212) 642-4900.

Material Data Sheet for Wood Executive Office and Conference Room Furniture

TO BE COMPLETED FOR ALL OFFERED LINES (OR SINGLE PIECES IF OFFERED SEPARATELY AS AN ACCENT OR SPECIALTY ITEM).  If a line is offered in more than one wood species, a separate material data sheet must be completed for each.

If an offeror offers only conference room furniture with no drawers, it is not necessary to complete the drawer portion of the material data sheet.

If a line is offered in more than one species, a separate check list must be completed for each.

Solicitation number:   ______________________________________

Offeror’s Name___________________________________________   Date:_________________

Furniture manufacturer’s name (if different from offeror):_________________________________

Name (or number) of line offered:___________________________________________________

Design (Traditional (A), Transitional (B), Contemporary (C):______________

Note:  When specifying the species of a wood, use the botanical name of the species and put the common name in parentheses (e.g. Prunus-Serotina (Cherry), Quercus Alba (White Oak)).

Chassis Construction

- Overall case construction Material: (e.g. Solid, Veneered panel with suitable core):

___________________________________________________________________________________

If solid construction, specify each solid wood species used for exposed parts, and where they are used: ____________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

If veneered panel construction, specify each face veneer species used for exposed parts (e.g. Prunus-Serotina (Cherry), Quercus Alba (White Oak))and where they are used: ________________________________________________________________________________________________________________________________________________________________________

- If veneered panel construction, specify core material used.  (e.g. Particleboard, MDF, Lumber core, Veneer Core):  __________________________

- If veneered panel construction, top panel edgeband species: _____________________

Top Edgeband Thickness: ___________

- If veneered panel construction, end panel edgeband species: _______________

End panel edgeband Thickness: ___________

- Panel molding material (when used)(e.g. solid wood, composite): ___________________

- If panel molding is solid wood, indicate species used (e.g. Prunus-Serotina (Cherry), Quercus Alba (White Oak): _____________________

- Base rail construction (e.g. solid wood, wood veneered): _____________________

- Exposed base rail wood species: ______________________

Veneer species, solid species, decorative surface used on:

Kneespace end panels: __________________________________________________________

Kneespace modesty (interior face) panel: ____________________________________________

Bookcase end panels (interior face): ________________________________________________

Bookcase back panel (interior face): ________________________________________________

Cabinet end panels (behind doors): _________________________________________________

Cabinet back panel (behind doors): _________________________________________________

Drawer Construction

Drawer Front

- Drawer front material & species (e.g. Solid Walnut, Veneered panel with Walnut face):

___________________________________________________________________________

- Edgeband material of veneered drawer front (e.g. wood edgeband, veneer edgeband, visible lumber core, foil, finished/printed MDF, P.V.C., N/A):

___________________________________________________________________________

- Wood species of drawer front edgeband and edgeband thickness (e.g. Walnut-3 mm, Cherry-0.6 mm veneer, N/A):

___________________________________________________________________________

## Drawer Sides and Back

- Drawer side material (e.g. solid wood, veneer core plywood, particleboard core plywood, vinyl wrapped MDF):

___________________________________________________________________________

- Drawer side overlay if not solid wood (e.g. wood veneer, vinyl, printed, N/A):

___________________________________________________________________________

- Drawer side solid wood or face veneer species (e.g. Beech, N/A):

___________________________________________________________________________

## Drawer Bottom

- Drawer bottom material (e.g. Wood veneered panel, printed hardboard, vinyl covered hardboard):

___________________________________________________________________________

- Drawer bottom face veneer species (e.g. Walnut, N/A):

___________________________________________________________________________

## Drawer suspension type (e.g. precision ball bearing, roller guide):

## ___________________________________________________________________________

Environmental Attributes:

List and include supporting documentation (See clause 552-238-72 and Environmental Attributes paragraph at beginning of schedule of items) for any product environmental attributes (e.g. certified woods, recycled content, low-emitting materials).

_______________________________________________________________________________

_______________________________________________________________________________

_______________________________________________________________________________